UNIVERSITY OF NAIROBI

SCHOOL OF ENGINEERING

DEPARTMENT OF ENVIRONMENTAL AND BIOSYSTEMS ENGINEERING

FEB 540: DESIGN PROJECT

DESIGN OF NATURAL BEEESWAX COATED FABRIC FOR TOMATO POST HARVEST QUALITY PRESERVATION CASE STUDY ROMBO AREA, LOITOKTOK SUB COUNTY

NAME

: BEATRICE NYAMBURA KIMANI

REGISTRATION NUMBER

: F21/2245/2017

SUPERVISOR

: DR. DUNCAN O. MBUGE

COURSE COORDINATOR

: ENG. MUTULI DANIEL A.

A project submitted in partial fulfillment of the requirements in the award of a degree in Bachelor of Science in Biosystems Engineering of the University of Nairobi

May2021

DECLARATION

I declare that this is my original work and has not been submitted for a degree award in any other university.

Beatrice N. Kimani

signature………………………………….

Date………………………………………

This report has been submitted for examination with the approval as a university supervisor

Supervisor:

Dr. Duncan O. Mbuge

signature…………………………………….

Date………………………………………….

i

ACKNOWLEDGEMENT

First and foremost, I would love to thank God Almighty without Him none of this would have been possible. I wish to acknowledge remarkable assistance and support of various people who have made the realization of this project through their various contributions, instrumental ideas and support.

I would like to express my gratitude towards my supervisor Dr. Duncan O. Mbuge for guiding me throughout the project by giving his endless contribution through constructive critics and his general willingness to give advice.

I also owe my extreme gratitude to my family especially my parents for their tireless effort to my academics endeavor, the lectures, support staff and also my fellow classmates. I could not have done it without you.

ii

DEDICATION

I would love to dedicate this project to both my parents, Mr. & Mrs. Kimani for seeing me through all those years in schooling and never once giving up on me.

iii

ABSTRACT

This report was prepared for the University of Nairobi as required for the undergraduate degree program in Environmental and Biosystems Engineering. It is aimed at shelf life extension and quality optimization of the tomato fruit.

With the specific objective being to design a solar wax melter to render beeswax as a raw material, design the natural coated beeswax fabric and design the ideal tomato box

The report has been systematized in different chapters. The introduction which provides an overview of the problem being addressed and the technology to be used.

Literature review about the properties of beeswax, extraction of beeswax using different techniques and on the tomato quality preservation.

Theoretical framework which looks at various design parameters of the design of the replicated box, wax solar melter and tomato pertinent parameters.

The methodology which has been applied to realize the objectives outlined by applying different formulae in order to come up with parameters in name.

Results and analysis that have been calculated using the methodology described in methodology and the data acquired. The design parameters discussion, conclusion and recommendations.

iv

| 1 | Contents |  |  |
| --- | --- | --- | --- |
| ACKNOWLEDGEMENT .............................................................................................................. | ii |
| DEDICATION ............................................................................................................................... | iii |
| ABSTRACT | ................................................................................................................................... | iv |
| LIST OF ABBREVIATIONS ...................................................................................................... | viii |
| List of figures ................................................................................. | Error! Bookmark not defined. |
| List of tables | ................................................................................... | Error! Bookmark not defined. |
| 1 | INTRODUCTION .................................................................................................................. | 1 |
|  | 1.1 | Background information .................................................................................................. | 1 |
|  | 1.2 | Problem Statement ........................................................................................................... | 3 |
|  | 1.3 | Problem Justification ........................................................................................................ | 4 |
|  | 1.4 | Site analysis and inventory ............................................................................................... | 5 |
|  | 1.4.1 | Location and map ...................................................................................................... | 5 |
|  | 1.4.2 | Climatic conditions ................................................................................................... | 6 |
|  | 1.4.3 | Population distribution .............................................................................................. | 7 |
|  | 1.5 | Objectives ......................................................................................................................... | 7 |
|  | 1.5.1 | Specific objectives .................................................................................................... | 7 |
|  | 1.6 | Statement of scope ........................................................................................................... | 8 |
| 2 | LITERATURE REVIEW ....................................................................................................... | 9 |
|  | 2.1 | Consumers’ interest in food safety, nutrition ................................................................... | 9 |
|  | 2.2 | Rationale for Using Edible Coating and Surface Treatments | .......................................... 9 |
|  | 2.3 | Beeswax as an organic preservative ............................................................................... | 11 |
|  | 2.4 | Permeability Properties of Coatings ............................................................................... | 13 |

v

|  | 2.4.1The influence of chemical composition and structure of the film-forming polymer |
| --- | --- |
|  | on film permeability .............................................................................................................. | 13 |
|  | 2.5 | Structural Integrity and Appearance of Coated Products ............................................... | 15 |
|  | 2.6 | Effect of coating on Gas Exchange of Fresh Fruits and Vegetables .............................. | 15 |
|  | 2.7 | Retardation of Weight Loss and Surface Dehydration................................................... | 16 |
|  | 2.8 | Evaporative Cooling ....................................................................................................... | 16 |
|  | 2.9 | Generation of beeswax from honeycomb....................................................................... | 17 |
|  | 2.9.1 | Traditional hives ..................................................................................................... | 18 |
|  | 2.9.2 | Modern beehives ..................................................................................................... | 20 |
|  | 2.10 |  | Wax extraction techniques .......................................................................................... | 24 |
|  | 2.11 |  | Quality of wax ............................................................................................................ | 27 |
|  | 2.12 |  | Preservation of tomato ................................................................................................ | 28 |
|  | 2.12.1 Commonly used methods for tomato preservation ................................................. | 28 |
|  | 2.13 |  | Tomato quality deterioration ...................................................................................... | 30 |
|  | 2.13.1 | Physiological deterioration ..................................................................................... | 30 |
|  | 2.13.2 | Mechanical deterioration ........................................................................................ | 31 |
|  | 2.13.3 | Microbiological deterioration ................................................................................. | 31 |
|  | 2.14 |  | The post-harvest handling systems of tomato ............................................................ | 32 |
| 3 | THEORETICAL FRAMEWORK ........................................................................................ | 34 |
|  | 3.1 | Solar wax Melter parameters.......................................................................................... | 34 |
|  | 3.2 | Pertinent parameters ....................................................................................................... | 34 |
|  | 3.3 | Wooden box design ........................................................................................................ | 34 |
| 4 | METHODOLOGY ............................................................................................................... | 36 |
|  | 4.1 | Determination of wax solar melter parameters .............................................................. | 36 |

vi

|  | 4.2 | Determination of beeswax properties ............................................................................. | 37 |
| --- | --- | --- | --- |
|  | 4.3 | Determination of the most suitable box design .............................................................. | 37 |
|  | 4.4 | Determination of tomato parameters .............................................................................. | 37 |
| 5RESULTS OF THE DESIGN PROJECT ............................................................................. | 39 |
|  | 5.1 | Site assessment ............................................................................................................... | 39 |
|  | 5.2 | Wax solar parameters ..................................................................................................... | 39 |
|  | 5.3 | Beeswax properties ........................................................................................................ | 40 |
|  | 5.4 | Design Calculations........................................................................................................ | 40 |
|  | 5.5 | Tomato parameters ......................................................................................................... | 41 |
|  | 5.6 | Bill of quantities ............................................................................................................. | 42 |
|  | 5.7 | Gross margin analysis .................................................................................................... | 43 |
|  | 5.8 | Economics of the project ................................................................................................ | 45 |
| 6 | DISCUSSION ....................................................................................................................... | 47 |
| 7 | CONCLUSIONS AND RECOMMENDATIONS ............................................................... | 48 |
|  | 7.1 | CONCLUSIONS ............................................................................................................ | 48 |
|  | 7.2 | RECOMMENDATIONS ............................................................................................... | 48 |
| References ..................................................................................................................................... | 49 |

vii

LIST OF TABLES

Table 2. 1: Tomato ripening	28

Table 5. 1: Comb properties	40

Table 5.2: Duration of tomato ripening- Box without the wax	41

Table 5.3: Duration of tomato ripening- Box with the wax	42

Table 5. 4: Bill of quantities	42

Table 5. 5: Gross margin analysis	43

Table 5.6: Economics of the project	45

viii

LIST OF FIGURES

Figure 1. 1: Ripening Span	3

Figure 1. 2: Tomato farmers in Rombo Area	4

Figure 1. 3: Project location	5

Figure 1. 4: Project site	6

Figure 1. 5: Average rainfall in Rombo Area	6

Figure 1.6: Average temperature in Rombo area	7

Figure 2. 1 : Process of Evaporating cooling	17

Figure 2. 2: Log hive	20

Figure 2. 3: Modern bee hive	21

Figure 2. 4: The top-bar hive	22

Figure 2. 5: The V-shaped top-bar	22

Figure 2.6: The Kenyan top-bar hive	23

Figure 2. 7: Honey extractor	24

Figure 2. 8: Wax solar melter	26

Figure 2. 9: Wax manual press	27

Figure 2. 10: Color of honeycomb	27

ix

LIST OF EQUATIONS

Equation 3.1	34

Equation 3.2	34

Equation 3.4	35

Equation 5. 1	45

Equation 5. 2	45

Equation 5. 3	46

x

LIST OF ABBREVIATIONS

SDG –Sustainable Development Goal

xi

1	INTRODUCTION

1.1	Background information

The tomato is one of the most consumed produce and the preservation of its shelf –life extension and quality is a continuous challenge. It is a climacteric fruit whereby it displays a well characterized peak in ethylene production and respiratory activity at the onset of ripening thus making it a very perishable produce whose shelf life is less than two weeks. There have been several attempts in its preservation to control post-harvest disease and maintain the quality of the fruit.

Moreover, many farmers in Kenya lack refrigeration facilities for their produce once it has been harvested and this is a major contributor to post harvest loss due to lack of access to electricity and how expensive it is. This is because most of them are low income earners and the lack of cooling makes it difficult for fresh produce to last, leading to massive food waste. Also, most market places located in Kenya lack a means of way to store their produce once it reaches the market and the disposal of the produce leads to environmental degradation. Majority rely on the outdated systems of conservations that eventually affect the texture firmness, color and also reduces the shelf-life of produce. This directly impacts on the sales and subsequent profit reduction. Let’s take a market vendor in Soko mjinga, Kibera who stores her spinach by sprinkling water on them and covers them with a light ‘gunia’ at the end of day. It takes two days before the spinach cannot be sold because it has rotten before its discarded therefore incurring losses.

On the other hand, the beeswax technology is not only affordable but can also be modelled to suit specific interests of the person of interest. A solar wax extractor works best when it comes to rendering beeswax. It can be made from almost any materials found around. The melter produces wax of high quality and eliminates the need for the sometimes hazardous job of rendering wax in the home.

Apart from its relevance in enhancing sustainable environment, it is also economical. Additionally, it has natural properties such as the antimicrobial, water resistant, and longevity, which makes it an excellent choice for this project. These wraps may not instantly reverse the

1

environmental pollutions that are currently at the peak levels, but they constitute smaller ways of putting brakes and halts on the continuous wastes as world strives for viable and lasting solutions. As such, the technology will enhance longevity because reports suggest that they can last anywhere between six to twelve months reducing the carbon footprint.

The wrap is made by infusing cotton cloth with beeswax and either jojoba oil or coconut oil. The beeswax is a naturally antibacterial and better at preserving moisture. By preserving moisture, microorganisms will not grow below a certain water activity (aW). The effect of excess moisture on the stability and quality of foods is subject to rapid deterioration from mold growth, heating, insect damage, and sprouting. The rate of browning of dehydrated vegetables and fruits and of oxygen absorption increases with an increase in moisture content.

The beeswax wrap is breathable allowing gases that spoil produce to escape allowing the produce to stay fresher for longer. These gases that accelerate deterioration of a produce are emitted to stimulate ripening. Ethylene gas (C2H4) is produced by fruits and some vegetables and is commonly referred to as an aging hormone. It is very harmful to vegetables since it kills the vegetable especially when it’s damaged. It is therefore recommended not to store vegetables and fruits together. Carbon dioxide (CO2) is also emitted when the fruit ripens to slow down the process of ripening. Some fruits in the supermarket such as apples are stored in controlled CO2 rooms to extend its shelf-life.

The antibacterial factor prevents microbial spoilage; activity of microbes that contaminate the produce; by inhibiting viable cell count of bacteria. This implies that it can constrain spread of food –borne bacterial pathogens and contribute to prevention of food spoilage.

According to a study conducted by Pinto, Pankoswki and Nano for the Journal of Microbiology, Biotechnology and Food Sciences on the anti-microbial activity of beeswax wraps against bacteria, fungi and viruses; tests that were done to check on the anti- bacterial activity using both Salmonella enteritidis, a gram-negative bacterium, and Staphylococcus aureus, a gram-positive bacterium, showed that there was decline on both cell and a decline in bacterial activity.

2